Specifications for

INSUL-TEK® Ductile Iron

A preinsulated piping system for above and below ground use on systems with temperatures up to

225⁰ F.

MATERIALS:

All pipe shall be factory preinsulated INSUL-TEK® Ductile Iron, as manufactured by

Insul-Tek® Piping Systems, Inc.

Carrier Pipe:

Pipe shall be ductile iron manufactured in accordance with the requirements of ANSI/AWWA C151/A21-51.  Push-on joints and mechanical joints for such pipe shall be in accordance with ANSI/AWWA C11/A21.11 and shall be based on laying conditions and internal pressure as specified in the project plans.  Any type of Ductile Iron Pipe commercially available may be utilized depending on customers preference.

INSULATION:

Foamed in-place closed cell polyurethane foam completely filling the annulus between the carrier pipe and jacketing.

Typical Mechanical Properties

Core Density

2.1 P.C.F., ASTM D-1622

Closed Cell Content

90 to 95%                ASTM D-2856

“K” Factor, BTU/hr.in/ft²/⁰F @ 73⁰ F

.16                       ASTM C-518

OUTER CASINGS:

HDPE:

Black High Density Polyethylene

Resin Type III, Grade P34,

Under ASTM D-1248

Tensile Yield Strength

3300 psi ASTM D-638

Ultimate Elongation

850%    ASTM D-638

Tangent Flexural Modulus

175,000 psi ASTM D-790

FRP:

Fiberglass Reinforced Plastic (FRP) comprised of isophthalic polester resin and fiberglass strand.  Minimum wall thickness to be a minimum 100 mils.  Vinylester resin is also available.  Please consult factory for recommendation.

Spiral Lockseam:

Galvanized Steel, Aluminum, Stainless Steel with standard outer lockseam.

*For optional casings, consult the Casing Selection Guide.